## Slide 1
Structural Integrity Issues at Repurposing Gas Pipelines for Hydrogen Service
Viacheslav Bogdanov 1, Zinoviy Nazarchuk 2, Olha Zvirko 2
1 S.P. Timoshenko Institute of Mechanics of the NAS of Ukraine
2 Karpenko Physico-Mechanical Institute of the NAS of Ukraine
2nd Olympiad in Engineering Science
OES 2025
Stavanger, Norway, June 10-14, 2025

## Slide 2
Prospects for the use of the Ukrainian gas transmission network for the transportation of green hydrogen
European Hydrogen Backbone vision – operating network of hydrogen pipelines in Europe by 2040
REPowerEU Plan – a plan to rapidly reduce dependence on Russian fossil fuels and fast forward the green transition
Europe’s goal by 2050 is to achieve a 13% share of hydrogen energy in the union’s energy balance
The construction of new dedicated hydrogen pipelines will be complemented with the repurposing of existing gas networks. According to the European Hydrogen Backbone, 70% could be repurposed by 2030.
The European Green Deal
2019
European Hydrogen Backbone
2020
REPowerEU
2022
Ukrainian natural gas transportation system
https://www.kmu.gov.ua
2
Hydrogen could play a key role in Ukraine’s green reconstruction and future development plans

## Slide 3
Ageing and in-service degradation of pipeline steels
Time of operation of gas transit pipelines
Effect of hydrogen blending on existing gas pipelines
Chart: 
| less 10 years | 11-32 years | 33-50 years | above 50 years
 | 0.432 | 9.006 | 16.818 | 6.832
 | 1 | 27 | 51 | 21
In-service degradation of pipeline steels
Influence of hydrogen on mechanical behaviour of pipeline steels
Issues at hydrogen transportation
Stages of operational degradation of pipeline steels
Deformation aging
Damage accumulation
3

## Slide 4
Ways of hydrogen charging
of steels
Hydrogen evolution
under corrosion
Dissociation
of molecular hydrogen
Steel pipe
HCO3- + e- = H + CO32-
H2 = H + H
Damage accumulation
Hydrogen uptake and damage accumulation in pipeline steels during their long-term service
Hydrogen assisted degradation of pipeline steels
H2О + e– = H + ОH–
SCC
Hydrogen
Crack branching due to delamination in rolling direction
In-bulk damaging of operated steels
4

## Slide 5
Steel | State | σys, MPa | σUTS, MPa | RA, % | δ, % | KCV, J/cm2 | JІС, MPa∙√m | CH, ppm
17H1S (eq. API 5L X52) | As-received | 378 | 595 | 79.0 | 20.2 | 200 | 322 | 1.6
 | Operated 29 years | 345 | 547 | 71.0 | 19.6 | 138 | 175 | 2.5
 | Operated 40 years | 302 | 515 | 69.0 | 26.3 | 125 | - | 3.6
API 5L X52 | As-received | 355 | 475 | 72,9 | 22.7 | 350 | 412 | 1.5
 | Operated 30 years | 261 | 455 | 63.4 | 21.9 | 186 | 127 | 1.9
 | Operated 30 years | 349 | 537 | 54.8 | 29.3 | 142 | 79 | 5.1
Relative changes in mechanical characteristics of API 5L X52 pipeline steels, caused by in-service degradation
Sensitivity of mechanical properties of steels to hydrogen assisted degradation
The most sensitive characteristics for an evaluation of in-service degradation of pipeline steels by destructive methods are fracture toughness and impact strength.
5

## Slide 6
Operational degradation of mechanical properties
Fracture surfaces of the operated steel specimens after the Charpy testing
Chart: 
| As-delivered state | Post-operated state
Longitudinal | 129 | 103
Transverse | 71 | 65
Steel state | Specimen type | KCV, J/cm2 | Jcr, N/mm
As-delivered | Longitudinal | 129 | 215.0
 | Transversal | 71 | 72.3
Post-operated | Longitudinal | 103 | 108.0
 | Transversal | 65 | 81.4
Longitudinal specimen
Transverse specimen
6
17H1S pipeline steel (0.17% C, 1.2% Mn), eq. API 5L X52, 38 years of operation

## Slide 7
Chart: 
| 0.05 | 1 | 0.05 | 1 | As-delivered state | Post-operated state
Longitudinal | 0 | 2.8 | 14.1 | 44.2
Transverse | 2.9 | 13.2 | 20.2 | 54.2
i, mA/cm2
Hydrogen embrittlement susceptibility
Hydrogen pre-charging:
Electrolyte – H2SO4 (pH1) + 10 g/l thiourea (NH2)2CS
1) i = 0.05 mA/cm2 (moderate mode)
2) i = 1 mA/cm2 (intensive mode)
Duration - 120 h
Post-operated steel
H pre-charged
7
Hydrogen embrittlement susceptibility
i = 0.05 mA/cm2 (moderate mode)
i = 1 mA/cm2 (intensive mode)
Cracking of non-metallic inclusions and defects in the structure of the operated steel after hydrogen charging
17H1S pipeline steel (0.17% C, 1.2% Mn), eq. API 5L X52,
38 years of operation

## Slide 8
Hydrogen embrittlement susceptibility
Fractographic signs of embrittlement
As-delivered steel
Post-operated steel
Without pre-charging
H-precharged at i = 0.05 mA/cm2
H-precharged at i = 1.0 mA/cm2
Typical SEM images of the fracture surfaces of the transverse specimens
8

## Slide 9
J – Δa curves of pipe steels for L–T and T–L specimens (displacement rate of 0.5 mm/min) without (1) and after hydrogen charging at i = 0.05 (2) and 1.0 mA/cm2 (3)
Reserve pipe
Operated for 38 years pipe
9
Longitudinal L-T
Longitudinal L-T
Transverse T-L
Transverse T-L
Reserve pipe
Operated for 38 years pipe
Hydrogen pre-charging in H2SO4 (pH1) + 10 g/l (NH2)2CS
Duration - 120 h
Hydrogen influence on fracture toughness of pipeline steels
Fractograms of the steel in (a, c) as-delivered and (b, c) operated states under fracture toughness tests of (a, b) L–T and (c, d) T–L specimens
17H1S pipeline steel (0.17% C, 1.2% Mn), eq. API 5L X52, 38 years of operation

## Slide 10
Steel state | Test condition | Displacement rate, mm/min |  | 
 |  | 0.5 | 0.05 | 0.005
As-delivered | Without hydrogen charging | 215.0 | - | -
As-delivered | Hydrogen pre-charged (i = 0.05 mА/cm2) | 117.2 | 92.5 | 77.5
Operated for 38 years | Without hydrogen charging | 108.0 | - | -
Operated for 38 years | Hydrogen pre-charged (i = 0.05 mА/cm2) | 75.6 | 60.3 | 43.6
Fracture toughness Jcr [N/mm] of the 17H1S steel, depending on its state, displacement rate and the influence of hydrogen (L-T specimens)
Chart: Jcr [N/mm]
| 0.05 mА/сm2 | 1.0 mА/сm2
As-delivered | 77.5 | 45.5
Operated | 43.6 | 32.1
HES of the 17H1S steel depending on the displacement rate of
L–T specimens after hydrogen charging under icat = 0.05 mА/сm2 and 1.0 mА/сm2
10
Hydrogen influence on fracture toughness of pipeline steels
Displacement rate - 0.005 mm/min

## Slide 11
Steel state | Envi-ronment | σUTS, MPa | σY, MPa | RA, % | KCV, J/cm2 | J0.2, N‧mm | βSCC, %
As-delivered state | Air | 531 | 428 | 71 | 129 | 322 | 
LTT |  | 535 | 433 | 72 | 125 | 330 | 
PEH + LTT |  | 533 | 435 | 74 | 131 | 286 | 
As-delivered state | NS4 solution | 529 | 429 | 69 | - | - | 3
LTT |  | 538 | 431 | 68 | - | - | 4
PEH + LTT |  | 537 | 434 | 53 | - | - | 25
Testing: The steel 17H1S (0.17% C, 1.5% Mn; API 5L X52) was studied in different states: 1) in the as-delivered state; 2) after low-temperature tempering (LTT) by keeping the samples at a temperature of 250°C for 1 h; 3) pre-electrochemically hydrogen charged (PEH) in H2SO4 (рН = 2) at і = 50 mA/cm2, 100 h followed by heating under the same mode (PEH + LTT) and holding 30 days in air for removal of diffusible hydrogen.
The studied steel after PEH + LTT is susceptible to SCC in NS4 solution
PEH + LTT
As-delivered state
Mechanical properties of the studied pipeline steel in different states
DSTU 9166:2021, strain aging: preliminary plastic deformation (10%) with the following heating to 250°C and holding 1 h.
Longitudinal direction
Transversal direction
Microstructure
Role of hydrogen-induced stresses in strain ageing of pipeline steels
11

## Slide 12
Hydrogen-induced defects in low-strength pipeline steels
The dominant mechanisms of hydrogen degradation in pipeline steels depending on the strength:
Crack initiation under hydrogen1
1M.C. Tiegel, et al., Acta Mater. 115 (2016) 24–34.
Strain rate in air 3·10-3 s-1; in NS4 solution - 3·10-7 s1
Steel Х70
Steel Х52
12
Hydrogen-deformation damaging in low-strength steel
Y/UTS < 0.7
Y/UTS > 0.8
0.7 < Y/UTS < 0.8
– Hydrogen-Induced Deformation
– Hydrogen-Induced Cracking
– Combination of different mechanisms
RASCC , RAair – reduction in area, determined by tensile testing in NS4 solution and air, respectively
Susceptibility to SCC in NS4 test solution:
As-delivered state
29 years of operation
Steel Х52

## Slide 13
Hydrogen-induced large-scale delamination in pipeline steels
Delaminations
Crack
Aboveground section of 30 years operated natural gas transit pipeline:
OD = 1420 mm,
t = 20 mm
OD = 219 mm, t = 18 mm
Steel Х60
The lateral pipelines of gas transit pipelines system, 40 years of operation
Pmax = 5.5 MPa
13
High pressure hydrogen

## Slide 14
Concluding remarks
14
Hydrogen assisted degradation of pipeline steels caused a deterioration of the mechanical properties and an increase in susceptibility to hydrogen embrittlement.
The implementation of the decohesive-deformation mechanism of damage in low-strength pipeline steels during long-term operation is substantiated, explaining an increase in hydrogen embrittlement susceptibility of long-term operated steels.
Hydrogen-induced stresses accompanied by dislocation generation are sufficient for strain aging of pipeline steels, which could occur under operation.
Using experimental studies of the fracture toughness of pipeline steels, determined by the J-integral method, a significant effect of the displacement rate of specimens on the values under hydrogen exposure is defined.
Aboveground natural gas pipelines are susceptible to hydrogen-induced large-scale delaminations.
Transportation of hydrogen via existing gas pipelines could enhance hydrogen charging of pipeline steels and, as a result, accelerate hydrogen assisted degradation, delamination and damage of pipeline steels, which can influence on the safe operation of pipelines and should be considered at assessment of the possibility of usage of the existing network for hydrogen transportation.

## Slide 15
Focus on the Ukrainian gas pipeline system but results potentially applicable to other systems
https://pgjonline.com/media/9912/hydrogen-pipe.jpg
15

## Slide 16
Olha ZVIRKO
​Prof., D.Sc., Corr. Member of the NASU, Head of Department
​E-mail: olha.zvirko@gmail.com
                Thank you for your attention!
The research has been partially financially supported by the National Academy of Sciences of Ukraine and the National Research Foundation of Ukraine under the Project No. 2022.01/0099
2nd Olympiad in Engineering Science
OES 2025
Stavanger, Norway, June 10-14, 2025
Karpenko Physico-Mechanical Institute of the National Academy of Sciences of Ukraine
Department of Diagnostics of Materials Corrosion-Hydrogen Degradation