## Slide 1
A Versatile Semi-Analytical Micromechanical Model for Elasticity of Cementitious Composites
Amit Kumar
&
Prof. Shashank Bishnoi
Indian Institute of Technology, Delhi

## Slide 2
Contents
Introduction
Literature Survey
Objectives
Methodology
Results
Conclusions

## Slide 3
Composites
  Materials made up of more than one substance that is used for building things.
Introduction
Applications:
✈️ Aerospace - Carbon fibre composites
🚗 Automotive - Lightweight body panels
🚀 Defence & Military - Bulletproof vests
🏗️ Civil Engineering & Construction - Reinforced concrete
🏥, ⚡, 🎾,… Many more
Why use composites:
High strength-to-weight ratio
Fatigue and corrosion resistance
Tailorable properties (e.g., directional stiffness)
Notes: Upto this- Why we need to study creep, Next why I am studying analytical modelling

## Slide 4
Reinforced concrete:
  An unpredictable multiscale composite
Introduction
Zhang, 2013
Constituent Properties
Curing
Mixing
Reasons of variability

## Slide 5
Approaches of prediction:
  Experiments : Can measure but do not predict. e.g. cube tests??
    Some phenomena like creep, fatigue, ASR are years-long.
  Empirical techniques: Based on macrostructural behaviour. Not generic.
A better approach: Utilize micro-structural behaviour
  FEM techniques:
    Great to model local behaviour.
    Time-costly for multi-level heterogeneity of concrete.
  Mean-Field Homogenisation Techniques
    Can analyse multi-level heterogeneity semi-analytically
    Less time consuming
    Microstructure is simplified but still useful.
Introduction

## Slide 6
Hashin, 1965
Definition: A homogeneous equivalent material storing same strain energy
Principle: The applied macroscopic strain/stress = Average of microscopic strains/stresses
= r and = r
Where, and
  , : Strain and Stress Concentration tensors
Effective Elastic Properties :
=
where =
Principle of homogenisation
Literature Survey
RVE

## Slide 7
Mori-Tanaka Scheme (Mori & Tanaka, 1973) | Self-Consistent Scheme (Hill, 1965) | Generalized Self-Consistent Schemes
The inhomogeneities are far from each other Effects are transferred through the matrix | The inhomogeneities are Near to each other Direct interaction of inhomogeneities | No distinct matrix exists e.g. a polycrystal material with grains in different orientations.
] |  | 
Mori-Tanaka Scheme (Mori & Tanaka, 1973) | Self-Consistent Scheme (Hill, 1965) | Generalized Self-Consistent Schemes
The inhomogeneities are far from each other Effects are transferred through the matrix | The inhomogeneities are Near to each other Direct interaction of inhomogeneities | No distinct matrix exists e.g. a polycrystal material with grains in different orientations.
Popular homogenisation methods
Literature Survey

## Slide 8
Levels | Levels | Constituents | Modelled shape | Remarks
Paste | C-S-H Gel | Solid C-S-H +Gel Pores | Spheroid (varying AR) Sphere | SCS used
 | C-S-H Foam | C-S-H Gel +Capillary Pores | Spheroid sphere | SCS used
Literature Survey
SCS is frequently used in cementitious systems
Hellmich, 2020
Sanahuja, 2007
Local reference frame needed

## Slide 9
Literature gaps
  Complicated techniques used for SCS.
  Not easy to comprehend and follow.
  Methods not versatile to be used across porosities aspect ratios
Objectives
  To devise a simpler method
  Versatile to work across for a range of porosities and aspect ratios
Konigsberger, 2020
Literature Gap & Objectives

## Slide 10
Methodology

## Slide 11
Methodology
Efficient calculations using Stroh- formalism
3x3x3x3 format requires 81 loops per tensor per iteration
6x6 format requires 36 loops per tensor per iteration

## Slide 12
Methodology
Nearest isotropic tensors
Bulk and shear moduli of nearest isotropic stiffness

## Slide 13
Results
Validation of the model

## Slide 14
Results
Effect of shape of solids
Oblate shapes appear to be most effective in increasing elastic modulus.
The effect of shapes of the solids reduce at upper scales: C-S-H gels, foam and the paste

## Slide 15
Conclusions
Model appears to be efficient and versatile for applying SCS on cementitious composites
Method of the nearest isotropic tensor using minimum Euclidean distance is useful.
Applicable to a wide range of aspect ratios and volume fractions.
Can predict the effect of aspect ratios and porosities
Easily extendible to other applications.

## Slide 16
Prof. Shashank Bishnoi

## Slide 17
Thank you for your Attention!
Amit Kumar
Ph.D. Scholar
Indian Institute of Technology, New Delhi, India
Email: amit.kumar@civil.iitd.ac.in
iitd.amitkr@gmail.com

## Slide 18
Complete Ph.D. Work
Multi-scale modelling of elasticity and creep of cementitious composites
A versatile model that works across different cementitious binders and water-cement ratios.
Link the creep observed in nano-seconds (as observed in indentation-creep tests) and over the years with a single model doe monotonic loading.
The effect of shape and constitutive properties of individual hydration products on the macro-level elastic and viscoelastic properties of cement pastes.
To estimate the effect of a change in capillary porosities on pastes' overall creep and elastic moduli.
To investigate the effect of the composition of C-S-H on the elastic modulus and creep of pastes.