## Slide 1: Assessing the Sustainability and Reuse Potential of Pre-fabricated Hollow Core Slabs: A Feasibility Study
Abhiram Sivapalakumar, Nirosha D. Adasooriya

## Slide 2: Rethinking Concrete in a Circular World
Concrete is the second-most used substance after water, with over 30 billion tonnes used annually.
~37% of the construction sector’s CO₂ emissions.
The cement industry is projected to fall short without advancement in technology sustainability—set to meet only half of the Paris Agreement targets.
pollution and resource depletion

## Slide 5: Wastage hierarchy
The primary target is to prevent wastage from occurring and then to control the wastage that has been made in a prioritized order.
Lack of guidelines has made it difficult to accomplish reusability so far.
Material recycling has been the main way to go.

## Slide 6: Recycled Concrete Aggregate (RCA)
Recycling is not a viable option!
Core Problem:
  RCA retains attached mortar, which brings in impurities:
    Glass, metal, dirt, plaster, gypsum, and other waste
  This leads to:
    Increased porosity
    Reduced mechanical strength
    Weakened bond with original aggregates
Practical Challenges:
  Cleaning requires extra steps:
    Water washing or air sifting
  Labour-intensive → higher costs
  No improvement in structural performance
Norsk betong 2016:
  Using RCA as a 20% replacement for natural aggregates may:
    Increase cement consumption
    Offset sustainability gains
Conclusion: Not yet viable for structural reuse without further innovation

## Slide 7: Cradle to grave (CtG)
Process: Extract → Use → Demolish → Waste
Results in:
  High embodied carbon loss
  Increased construction waste
  No material recovery
Still the industry norm in most life cycle assessments

## Slide 8: Cradle to Cradle (CtC)
Regenerative approach:
  Materials are reused, remanufactured, or repurposed
Key principles:
  Narrow resource loops (less input)
  Slow material flows (longer life)
  Close the loop (reuse/recycling)
To make it possible : Design for Disassembly (DfD)
  Allows safe, non-destructive dismantling
  Essential for reusing elements like HCSs
  Supports structural integrity across lifecycles

## Slide 9: Reusability
ISO 20887 defines reusability as the following:
“Ability of a material, product, component or system to be used in its original form more than once and maintain its value and functional qualities during recovery to accommodate reapplication for the same or any purpose”.
Literature study on previous reuse cases:
  Poland
  Kristian Augustus Road 13 (KA13)
  Oslo Storby Legevakt (OSBL)
  Norwegian firms survey
Advantages
Disadvantages
Often longer technical life span
Costly procedure (high initial cost)
Lack of proper documentation
Environmentally friendly
Technical challenges
Resource efficient
New market
Current regulations for reuse
Lack of clear and harmonized definition of reuse

## Slide 10
SIS- Velferds Bygg (SVB)

## Slide 11: Environmental benefits of HCS
Chart: GWP value of saved mass (SVB)
| HK | H1 | H2 | H3
GWP-total | 37702.668 | 47287.7961 | 25352.7381 | 38207.1513
Chart: Water usage Solid slab VS HCS
| HK | H1 | H2 | H3
Total mass Solid Slab | 44432.6598 | 55894.547 | 30355.3701 | 45112.0094
Total mass HCS | 25020.4484 | 31547.1799 | 17301.8453 | 25440.0514

## Slide 12: Case study introduction
SVB used HD265 and HD320 slabs
  1,898 tonnes of prefabricated concrete
Project Goal:
  Repurpose Hollow-Core Slabs (HCSs) from the SVB building
  Construct a new student housing facility
  Maximize material efficiency while meeting safety and comfort standards

## Slide 13
Selection & Planning
  Chosen: HD265 slabs, 8.4 m × 1.2 m
  Criteria:
    Minimal topping & damage
    Clean geometry
    High compatibility with new layout
  Total reused slab area: 1,098.37 m²
Integration in New Design
New floor plan: ~68.5 m × 18.5 m
  Functional spaces:20 m² student rooms
  Bathrooms, laundry, and shared areas
Support structure:L-shaped & Inverted Tee Beams
Used existing voids for anchorage, reducing extra drilling

## Slide 15: Environmental benefits of reusing HCS from SVB
System Limit | GWP-total (Unit: kgCO2-eq) | Percentage (%)
A1 | 34588,412 | 80,37
A2 | 244,525 | 0,57
A3 | 1088,529 | 2,53
A4 | 216,523 | 0,50
A5 | 4101,705 | 9,53
C1 | 1577,579 | 3,67
C2 | 485,105 | 1,13
C3 | 191,281 | 0,44
C4 | 540,321 | 1,26%
System Limit | GWP-total (Unit: kgCO2-eq) | Percentage (%)
E1 | 4101,705 | 42,18%
E2 | 216,523 | 2,23%
E3 | 1088,529 | 11,19%
F1 | 216,523 | 2,23%
F2 | 4101,705 | 42,18%
GWP total with CtG approach
GWP total with CtC approach

## Slide 16: Guidelines
Pre-Disassembly Evaluation
Disassembly Procedures
Testing and Evaluation
Documentation Strategy

## Slide 17: Pre-disassembly evaluation
Six key areas for evaluation
Access to elements:
  Visibility, accessibility, and building changes from original blueprints. Uses "access map".
Independence
  Can HCSs be removed without damaging other parts?
  Focus on connections and load paths.
Treatments & Finishes
  Are there adhesives, coatings, or sealants that hinder disassembly?
  Are they removable
Standardization
  Are dimensions, materials, and connections uniform?
  Standard = faster, safer, cheaper reuse.
Economic Appraisal
  CBA, NPV, IRR, payback period, and risk/sensitivity analyses—will reuse be cost-effective?
Environmental Impact
  Compare GWP, waste reduction, water/energy savings vs. traditional demolition.

## Slide 19: Disassembly procedure
What is Disassembly?
  The reverse of construction — but with resource efficiency, precision, and future reuse in mind.
Planning Before Execution
  Site Survey & Document Review (NS 3682 §5.1–5.2)
    Analyze slab positions, loads, and connections
    Identify potential hazards & supports needed
  Tool & Equipment Planning
    Cranes, lifting gear, cutting tools
    Avoid diagonal cuts – use straight cuts to minimize damage
  Disassembly Strategy
    Reverse the original assembly sequence
    Start with least load-bearing slabs, install temporary supports as needed

## Slide 20: Crane positioning is very important!

## Slide 21: Testing and evaluation
Three evaluation areas:
Technical Performance:
  Assess structural strength & serviceability
Functional Performance:
  Compliance with fire, sound, and system integration needs
Aesthetical Performance
  Visual quality & physical condition for reuse
Pass criteria:
  The technical lifespan must exceed both functional and aesthetic lifespans for reuse to be approved.

## Slide 22
Technical performance
Chemical degradation
Load-bearing capacity tests
Deflection check
Pre-tensioned wires/ RF
Functional performance
Compatibility assessment
Fire resistance
Sound insulation
Aesthetical performance
Visual control
Damage
Connections
Pre-tensioned wires/ RF

## Slide 23: Documentation of reusable HCS
Case studies (KA13, OSBL) show: Lack of documentation is a key barrier to HCS reuse.
Ensures traceability, compliance, and market acceptance
Aligns reused HCSs with CE-marked standards via NS 3682
If a reused product meets CE-equivalent standards in one EEA country, Norway must accept it (DOK §14)
Ensures smoother cross-border reuse with no redundant testing

## Slide 24
Thorough, standardized documentation is not just regulatory—it's a practical enabler of reuse at scale.

## Slide 25
NO
YES
Flowchart summarizing all guidelines

## Slide 26: Economic and social perspectives
Economic Challenges:
  High upfront costs
  Lack of incentives.
Potential Solutions:
  Carbon pricing
  Subsidies
  Green building certifications.
Social Impact:
  Public trust
  Community benefits
  Housing affordability
  job creation.