## Slide 2: Structural Performance and Load-Carrying Capacity of Cross Laminated Timber-Concrete Composite Slabs: Influence of Shear Fasteners
Maria Bergfjord1, Sudath C. Siriwardane2 and Lars Henning Krokengen3
1 Multiconsult AS, Oslo, Norway
2 University of Stavanger, 4036 Stavanger, P.O. box 8600, Norway
3 COWI AS, Trondheim, Norway

## Slide 3: Outline
Background
Research/Knowledge gaps
Objectives
Materials and test sample preparation
Laboratory testing
Theoretical prediction of load capacity and displacement
Discussion and comparison of the result
Conclusions

## Slide 4: 1. Background
Environmental impacts
Reinforced concrete
Timber
Usage of Cross Laminated Timber (CLT) relatively new

## Slide 5: 2. Research/Knowledge gaps
Limited Research on CLT-Concrete Composite Floor Systems
Absence of Standardized Design Guidelines
Limitations of Eurocode 5
Material Anisotropy and Defects
Insufficient Research on Shear Fasteners

## Slide 6: 3. Objectives
To investigate the load capacity and structural response of 5-layeres CLT-concrete composite slabs with two different types of shear fasteners by medium scale laboratory testing
The validity of the modifications to the existing formulas in the Eurocode is investigated for theoretical prediction of 5-layered CLT-concrete composite slabs as a secondary objective of this paper.
10. A. Gustafsson + et al., “The CLT handbook CLT structures - facts and planning”,
1. Ed, Stockholm: Skogsindustrierna, 2019

## Slide 7: 4. Materials and test sample preparation
Cross Laminated Timber (CLT)
Concrete B35
  Self-compacting concrete (SCC)
  Quality check
Shear fasteners
  CTC screw – SLAB type A
  KOP screw – SLAB type B
Formwork and casting
Curing and demoulding
SLAB Type B
SLAB Type A

## Slide 8: 5. Laboratory testing
Test setup
Four point bending test
  NS-ISO 6891:1991 Timber structures – Joints made with mechanical fasteners
Trekonstruksjoner Mekaniske forbindelsesmidler
Generelle prinsipper for bestemmelse av styrke og
deformasjonsegenskaper (= EN 26891:1991) (ISO 6891:1983), NS-ISO 6891:1991

## Slide 9: 5. Laboratory testing (con.) - Test result
SLAB | LOAD CAPACITY (kN) |  |  |  | MAXIMUM DISPLACEMENT (mm) |  |  | 
 | 1ST DROP | 2ND DROP | 3RD DROP | MAX | 1ST DROP | 2ND DROP | 3RD DROP | MAX
A1 | 107.16 | - | - | 226.60 | 6.16 | - | - | 25.03
A2 | 128.30 | 138.25 | 210.85 | 229.75 | 7.67 | 8.99 | 20.65 | 28.80
A3 | 124.25 | 133.62 | - | 245.96 | 6.86 | 8.07 | - | 26.01
A4 | 120.73 | 124.37 | - | 207.96 | 6.99 | 8.24 | - | 26.15
A5 | 114.69 | - | - | 171.63 | 8.59 | - | - | 15.86
A6 | 130.17 | 148.41 | - | 188.12 | 8.80 | 11.70 | - | 24.28
B1 | 72.40 | - | - | 191.88 | 5.04 | - | - | 26.91
B2 | 82.29 | - | - | 144.19 | 5.58 | - | - | 13.03
B3 | 85.96 | - | - | 191.43 | 5.73 | - | - | 22.61
B4 | 96.49 | - | - | 181.12 | 6.59 | - | - | 23.20
B5 | 86.88 | - | - | 211.78 | 4.76 | - | - | 22.69
B6 | 104.08 | - | - | 239.94 | 5.43 | - | - | 23.20

## Slide 10: 5. Laboratory testing (con.)
Load-deflection response for slab A1-A6
Load-deflection response for Slab B1-B6

## Slide 11: 6. Theoretical prediction of load capacity and displacement
𝜸−method
  Mechanically jointed beams theory
  Limitations : 2/3 layered TCC
  Effective bending stiffness based on composite action
Clause B.2: EC 1995-1-1:2004+A1:2008+NA2010

## Slide 12: 6. Theoretical prediction of load capacity and displacement (con.)
Shear analogy method
  Glued not nailed CLT
  No limitations to lamellae or shear fastener type
  The different moduli of elasticity of a single layer
  Shear deformation in longitudinal and transverse layer
B. Douglas and E. Karacabeyli, “Structural design of cross laminated timber elements,”
in CLT Handbook – cross-laminated timber, US ed. Pointe-Claire,
QC, Canada: Library and Archives Canada Cataloguing in Publication, 2013, Chapter 3, p. 11

## Slide 13: 6. Theoretical prediction of load capacity and displacement (con.)
Short-term verification
Long-term verification
Alternative theoretical verification

## Slide 14: 6. Theoretical prediction of load capacity and displacement (con.)
TYPE OF THEORETICAL APPROACH | SHORT-TERM |  |  |  | LONG-TERM |  |  | 
 | LOAD CAPACITY (kN) |  | DISPLACEMENT (mm) |  | LOAD CAPACITY (kN) |  | DISPLACEMENT (mm) | 
 | A - CTC | B - KOP | A - CTC | B - KOP | A - CTC | B - KOP 3 | A - CTC | B - KOP
CONVENTIONAL APPROACH | 75.68 | 82.96 | 5.61 | 5.73 | 117.65 | 115.52 | 17.91 | 18.51
FAILURE OF TOP CLT (M3) | 136.52 | 133.90 | 9.86 | 10.13 | 188.88 | 116.04 | 18.34 | 18.82
FAILURE OF BOTTOM CLT (M4) | 177.93 | 166.44 | 14.36 | 13.82 | 153.93 | 143.62 | 26.33 | 25.41
CONVENTIONAL APPROACH USING B45 CONCRETE STRENGTH | 94.35 | 91.99 | 6.86 | 26.33 | 120.07 | 117.23 | 18.33 | 18.81
CONVENTIONAL APPROACH USING AVERAGE CONCRETE STRENGTH | 136.51 | 133.90 | 9.85 | 25.41 | 118.88 | 116.03 | 18.34 | 18.82

## Slide 15: 7. Discussion and comparison of the result
Observed failure scenarios
Limitations
Comparison of the theoretical and experimental results

## Slide 16: 7. Discussion and comparison of the result (con.) - Observed failure scenarios
Finger joint and knot failure in the timber
Cracks in both timber and concrete
Stability of slab A with CTC screws after four point bending test
Stability of slab B with KOP screws after four point bending test

## Slide 17: 7. Discussion and comparison of the result (con.) - Limitations of provided material
Concrete mix
Definition of failure
Theoretical vs. experimental predictions – long term
Correct orientation of lamellae
Incorrect orientation of lamellae
Length
SLAB | LENGTH
A2 | 2.068 m
A3 | 2.067 m
B5 | 2.069 m
C1 | 2.068 m

## Slide 18: 7. Discussion and comparison of the result (con.) - comparison of theoretical predictions and experimental result
SLAB | DEFLECTION FOR NO COMPOSITE DN (mm) | DEFLECTION FOR FULL COMPOSITE DC (mm) | DEFLECTION MEASURED IN LAB TEST DI (mm) | EFFICIENCY (%)
A1 | 5.547 | 5.612 | 6.160 | 9.616
A2 | 5.547 | 5.612 | 7.673 | 33.367
A3 | 5.547 | 5.612 | 6.859 | 20.586
A4 | 5.547 | 5.612 | 7.000 | 22.765
A5 | 5.547 | 5.612 | 8.586 | 47.963
A6 | 5.547 | 5.612 | 8.803 | 51.102
B1 | 6.354 | 5.725 | 5.037 | 2.094
B2 | 6.354 | 5.725 | 5.579 | 1.233
B3 | 6.354 | 5.725 | 5.730 | 0.993
B4 | 6.354 | 5.725 | 6.591 | -0.3767
B5 | 6.354 | 5.725 | 4.760 | 2.535
B6 | 6.354 | 5.725 | 5.436 | 1.466

## Slide 19: 7. Discussion and comparison of the result (con.) - comparison of theoretical predictions and experimental result

## Slide 20: 8. Conclusion
Key finding
  The load-displacement response
  Theoretical predictions vs. laboratory testing
Recommendations
  Additional testing with same five-layer CLT, concrete strength and fasteners type
  Enhanced instrumentation for slip behaviour (strain gauges)
  Further studies with exploring variations in fasteners type, spacing etc.

## Slide 21: Acknowledgements
Jarle Berge, Samdar Kakay, Jan-Tore Jakobsen and Andreas Skaare – UiS
Eugenio Facchini, technical sales consultant in Rothoblaas