## Slide 1: Dynamics of Ionic liquids confined in porous glasses – a showcase for pA in QENS
July 2025 I o. holderer (JCNS)

## Slide 2: MLZ – View into the Neutron guide hall
MLZ virtual visit:
https://mlz-garching.de/panorama/full/de/index.html

## Slide 3: Relevant Time- and lengthscales
http://europeanspallationsource.se/feature-series-ess-instrument-suite

## Slide 4: Correlation function
Time
q (inverse length scale)
q=2p/d

## Slide 5: Correlation function
Time
q (inverse length scale)
q=2p/d

## Slide 6: Neutron spin echo spectroscopy
S. Pasini et al., Rev. Sci. Instr. (2019)
P.A. Zolnierczuk, J. Appl Cryst. (2019)

## Slide 7: Wide angle NSE: WASP

## Slide 8: EMIM Ac and porous glasses
How does confinement in porous glasses influence the IL structure and dynamics?
1-ethyl-3-methylimidazolium acetate

## Slide 9: Confined lamellar structure
0.5 molar H2O to IL
X-ray diffraction: Broad peak with characteristic length scale similar to sponge phase
Fit with Teubner-Strey function
In confinement: increased correlation length
Lamellar ordering
D. Noferini, O. Holderer, H. Frielinghaus, Phys. Chem. Chem. Phys. (2020) 22, 9046
H. Frielinghaus, ...,OH, Frontiers in Physics (2022) 10, 872616

## Slide 10: Confined lamellar structure

## Slide 11: Intensity
Mixed coherent and incoherent scattering
Here: focus on incoherent scattering only

## Slide 12: I(Q,t)
Hydrogen motion captured in t1.
Other contributions mainly elastic on the time scales of the experiment.

## Slide 13: RESULTS
Diffusion of H2O follows mainly acetate dynamics
Slight reduction of activation energy in confinement
H2O in low concentration (0.5 molar) strongly linked to ionic liquid
Molecular mixture of water and acetate

## Slide 14: picture
D. Noferini, O. Holderer, H. Frielinghaus, Phys. Chem. Chem. Phys. (2020) 22, 9046
H. Frielinghaus, ...,OH, Frontiers in Physics (2022) 10, 872616
Bulk IL
At interface
Confinement:
Induced lamellar structure
Reduced activation energy
Water addition:
Little influence on proton dynamics

## Slide 15: What about coherent scattering? High Q

## Slide 16: Intensity and polarization
NSE:
BS:
Complementary information from NSE and BS

## Slide 17: Separation of contributions
Hypothetical scenarios:

## Slide 18: Conclusion
Insight into dynamics under confinement from QENS
Wide Angle Spin Echo provides right time-scale data analysis involved due to coherent/incoherent contributions
Interfaces affect structure and diffusion
Backscattering provides complementarity, especially with polarization analysis

## Slide 19: Acknowledgement
ILL local contacts from WASP: Peter Falus Peter Fouquet
Jülich Deuteration Lab: Lisa Fruhner
JCNS at MLZ: Henrich Frielinghaus Margarita Fomina Dominic Hayward Purushottam Dubey Sebastian Jaksch

## Slide 20
June 15-19, 2026
go.fzj.de/neutronsandfood8

## Slide 21: Structure
D. Noferini, O. Holderer, H. Frielinghaus, Phys. Chem. Chem. Phys. (2020) 22, 9046
X-ray diffraction:
IL: Broad peak with
characteristic length scale similar to sponge phase
Fit with Teubner-Strey function
In confinement: increased correlation length
Lamellar ordering

## Slide 22: Neutron Backscattering spectroscopy: S(q,E)
Self correlation function:
Hopfenmüller et al, JCP 2018

## Slide 23: Phase behaviour: elastic scans and DSC
Help from Jia-Jhen Kang (TU München) for the DSC measurements is acknowledged
D. Noferini, O. Holderer, H. Frielinghaus, Phys. Chem. Chem. Phys. (2020) 22, 9046

## Slide 24: S(q,E)
D. Noferini, O. Holderer, H. Frielinghaus, Phys. Chem. Chem. Phys. (2020) 22, 9046
Neutron backscattering spectroscopy at SPHERES (MLZ)
Bulk VP AGC

## Slide 25: Diffusion in confinement
D. Noferini, O. Holderer, H. Frielinghaus, Phys. Chem. Chem. Phys. (2020) 22, 9046
Singwi-Sjölander jump diffusion model:
Jump length l and residence time t
Larger effects of confinement at higher T