## Slide 1
Phonon Dynamics of CsAg5Te3-based Thermoelectric Materials by Combining First-principles and Neutron Scattering
Institute of High Energy Physics, Chinese Academy of Sciences
Spallation Neutron Source Science Center
Bao-Tian Wang (王保田)
PAQMAN2025

## Slide 2
1
2
Background
Neutron Scattering and DFT Calculations of CsAg5Te3
3
Computational study of α–CsCu5Se3
4
Neutron Scattering and DFT study of CsCu4Se3
Contents

## Slide 3
1. Background
Merits:
Thermal-to-electric energy conversion and vice versa
Small volume and light mass
Small ∆T for temperature control
Environment friendly
Thermelectric Materials

## Slide 4
Two main mechanisms for low lattice thermal conductivity (κL) of high-performance thermoelectric materials:
Giant Anharmonic Phonon Scattering
SnSe、SnTe、PbTe
2. Suppressing Phonon Scattering by Disordered Structures
CuCrSe2、AgCrSe2、CsAg5Te3
1. Background
Nat. Phys., 2015, 11, 1063; Nat. Mater., 2011, 10, 614; Nat. Mater., 2018, 17, 226; Nat. Phys., 2019,15, 73.

## Slide 5
Nat. Phys., 2015, 11, 1063; Nat. Mater., 2011, 10, 614; Nat. Mater., 2018, 17, 226; Nat. Phys., 2019,15, 73.
1. Background

## Slide 6
α-MgAgSb:
Room-temperature TE material
Low κL
ZT up to 1.4 at 525 K
High conversion efficiency
1. Background
Nano Energy 2014, 7, 97; Adv. Funct. Mater. 2015, 25, 6478
X.Y. Li#, P.F. Liu#, B.T. Wang*, Z.F. Ren*, H.Z. Zhao*, F. Wang*, et al., Nat. Commun. 2020, 11, 942.

## Slide 7
Intrinsic Mg-Sb distorted rocksalt sublattice structure
Transverse Acoustic Phonons
Longitudinal Acoustic Phonons
Ultralow klat
1. Neutron scattering and DFT calculations on α-MgAgSb
X.Y. Li#, P.F. Liu#, B.T. Wang*, Z.F. Ren*, H.Z. Zhao*, F. Wang*, et al., Nat. Commun. 2020, 11, 942.
1. Background

## Slide 8
Experiments
High-temperature solid state reaction method
Spark plasma sintering (SPS)/Hot-pressed (HP) samples
Laser flash diffusivity method
Neutron Diffraction Measurements: CSNS@MPI
Inelastic Neutron Scattering (INS) Measurements: J-PARC@AMATERAS
DFT calculations
Ab initio calculations:
Harmonic phonons: Phonopy
Anharmonic phonons & κlat: Phono3py/TDEP/DynaPhoPy
S(Q,E) map: Euphonic
2. Neutron Scattering and DFT Calculations of CsAg5Te3

## Slide 9
The most key and remarkable features of CsAg5Te3：
1. Complex structure (large unit cell)
1. Ultralow κL (<0.2 Wm-1K-1@300K)
2. A constant κ (300~700 K)
3. High ZT >1.5@700 K (p-type)
4. Large optic-to-acoustic phonon ratio
Low-κL mechanism?
1. Neutron scattering
2. DFT calculations
2. Neutron scattering and DFT calculations on CsAg5Te3
2. Neutron Scattering and DFT Calculations of CsAg5Te3
Lin et al., Angew. Chem. Int. Ed. 55, 11431–11436 (2016).
Ma et al., J. Am. Chem. Soc., 142, 5293-5303 (2020).

## Slide 10
2. Neutron scattering and DFT calculations on CsAg5Te3
CsAg5Te3：High ZT >1.5@700K
2. Neutron Scattering and DFT Calculations of CsAg5Te3
P.F. Liu#, X.Y. Li#, Hua Lin*, J. Zhang*, J. He*, Bao-Tian Wang*, et al., Natl. Sci. Rev., 2024, 11, nwae216.

## Slide 11
Low-κ mechanism in CsAg5Te3?
Neutron scattering & DFT calculations
2. Neutron Scattering and DFT Calculations of CsAg5Te3
P.F. Liu#, X.Y. Li#, Hua Lin*, J. Zhang*, J. He*, Bao-Tian Wang*, et al., Natl. Sci. Rev., 2024, 11, nwae216.

## Slide 12
AMATERAS
Proposal No.: 2022A0304
2. Neutron Scattering and DFT Calculations of CsAg5Te3
Neutron-weighted phonon
calculated by DFT
S(Q,E)
P.F. Liu#, X.Y. Li#, Hua Lin*, J. Zhang*, J. He*, Bao-Tian Wang*, et al., Natl. Sci. Rev., 2024, 11, nwae216.

## Slide 13
2. Neutron Scattering and DFT Calculations of CsAg5Te3
Neutron-weighted phonon calculated by DFT
S(Q,E)
P.F. Liu#, X.Y. Li#, Hua Lin*, J. Zhang*, J. He*, Bao-Tian Wang*, et al., Natl. Sci. Rev., 2024, 11, nwae216.

## Slide 14
Neutron-weighted phonon calculated by DFT
2. Neutron Scattering and DFT Calculations of CsAg5Te3
P.F. Liu#, X.Y. Li#, Hua Lin*, J. Zhang*, J. He*, Bao-Tian Wang*, et al., Natl. Sci. Rev., 2024, 11, nwae216.

## Slide 15
2. Neutron Scattering and DFT Calculations of CsAg5Te3
Stable in wide temperature range of 8-700 K: No structural phase transition or superionic transition occurred;
The Ag-Te/Ag-Ag bonds exhibit significant softening behavior upon heating from 300 K to 500 K；
The liquid-like vibrational behavior of Ag ions induces strong phonon anharmonicity and ultralow κL.
P.F. Liu#, X.Y. Li#, Hua Lin*, J. Zhang*, J. He*, Bao-Tian Wang*, et al., Natl. Sci. Rev., 2024, 11, nwae216.

## Slide 16
2. Neutron Scattering and DFT Calculations of CsAg5Te3
P.F. Liu#, X.Y. Li#, Hua Lin*, J. Zhang*, J. He*, Bao-Tian Wang*, et al., Natl. Sci. Rev., 2024, 11, nwae216.

## Slide 17
3. Computational study of α-CsCu5Se3
Ref: Ma et al., J. Am. Chem. Soc., 142, 5293-5303 (2020).
CW
CW
CW

## Slide 18
Alamode-CSLD
(compressive sensing lattice dynamics)
3. Computational study of α-CsCu5Se3
Refs: Zhou et al., Phys. Rev. Lett., 113, 180511 (2014).
Simoncelli et al., Nat. Phys., 15, 809 (2019).
CSLD
Alamode
Phonopy
ShengBTE (Phono3py)
HiPhive

## Slide 19
3. Computational study of α-CsCu5Se3
Crystal structure and anharmonicity
The rattling modes associated with the Cu3 atoms are expected to play an important role in its phonon transport.
Qing-Yu Xie, Bao-Tian Wang*, et al., PRB, 2023, 108, 014302.

## Slide 20
3. Computational study of α-CsCu5Se3
Temperature-induced anharmonic phonon renormalization
Strong quartic anharmonicity of tetragonal α-CsCu5Se3 strongly hardens the low-energy phonon branches.
Qing-Yu Xie, Bao-Tian Wang*, et al., PRB, 2023, 108, 014302.

## Slide 21
3. Computational study of α-CsCu5Se3
Particle-like contributions to κL
The hardening effect diminishes the three-phonon scattering processes at finite temperatures.
Qing-Yu Xie, Bao-Tian Wang*, et al., PRB, 2023, 108, 014302.

## Slide 22
3. Computational study of α-CsCu5Se3
Wave-like contributions to κL
Strong phonon broadening leads to a strong coupling between interbranch coherent vibration eigenstates, manifested in glasslike κL and dominated by wave-like tunneling of phonons.
Qing-Yu Xie, Bao-Tian Wang*, et al., PRB, 2023, 108, 014302.

## Slide 23
3. Computational study of α-CsCu5Se3
Experiment:
Single crystal
Electronic thermal conductivity
Off-stoichiometry between various Cu atoms
Theory and computational:
Thermal expansion effect
Anharmonic contributions to heat-flux
Higher-order phonon linewidths
Relaxation time approximation (RTA)
Qing-Yu Xie, Bao-Tian Wang*, et al., PRB, 2023, 108, 014302.

## Slide 24
Qing-Yu Xie#, Xi-Yang Li#, Fei Jia#, Li-Ming Wu*, Bao-Tian Wang*, et al., in progressing
4. Neutron Scattering and DFT study of CsCu4Se3
Refs:
Ma et al., J. Am. Chem. Soc., 142, 5293-5303 (2020).
Ma et al., J. Am. Chem. Soc., 143, 18490-18501 (2021).
CW
CW
CW

## Slide 25
Structure and phonon dynamics in CsCu4Se3
Structure, PhDOS, and S(Q,E) at different temperatures.
NPD/INS/DFT
CSNS
Neutron scattering experiments:
CSNS@MPI Finished No. P1622120100031
J-PARC@AMATERAS Finished No. 2023B0040
4. Neutron Scattering and DFT study of CsCu4Se3
Qing-Yu Xie#, Xi-Yang Li#, Fei Jia#, Li-Ming Wu*, Bao-Tian Wang*, et al., in progressing

## Slide 26
4. Neutron Scattering and DFT study of CsCu4Se3
Unpublished
Unpublished
Unpublished
Unpublished
Qing-Yu Xie#, Xi-Yang Li#, Fei Jia#, Li-Ming Wu*, Bao-Tian Wang*, et al., in progressing

## Slide 27
(Magnetic) Structure
Phonon Dynamics
XRD
NPD
DFT
VASP/QE
USPEX
Calypso
MagGene
MD/MC
LAMPPS
UppASD
RIXS
INS
Raman
DFT/MD
LAMPPS/GUPMD
VASP/QE
ShengBTE
Phono3py
ALAMODE
Euphonic
OCLIMAXDynasor
Overall Planning
ML

## Slide 28
5 Acknowledgment
Dr. Peng-Fei Liu Dr. Qing-Yu Xie Dr. Xiyang Li

## Slide 29
d
Thanks!