## Slide 1: QENS Study of the interface dynamics IN HUMID iron oxide nanoparticles
04.07.2025 I Matei Pascariu

## Slide 2: Introduction & Scientific Motivation
Versatile
Interactions can be tailored by surface functionalization
Measuring Surface Dynamics with QENS
IN16B @ ILL in BS mode:
λ = 6.271 Å
energy-resolution HWHM ≈ 0.37 µeV
ΔE range ± 30 µeV
XPD
NPD
WOMBAT, ANSTO
TEM, © Sascha Ehlert, FZJ
20 nm
nm IONP
Q [Å-1]
I [a. u.]
Sample composition (85% RH)
≈ 15 wt% water and citrate
Hwater : Hcit = 2.81 : 1

## Slide 3: Citrate-Capped IONPs at 85% RH
FWS Analysis
A: water and ligand motions are largely “frozen”, magnetic process most noticeable at Q10
B: feature observable at higher Q values
C: possible phase transition in the hydration water, the dynamics here are optimally active
D: possible dynamics after the phase transition, qe component exits the spectrometer’s observable window
• 0.94 Å-1
• 1.31 Å-1 (Bragg peak)
• 1.62 Å-1
• 0.94 Å-1
• 1.31 Å-1 (Bragg peak)
• 1.62 Å-1
EFWS
IFWS (3 μeV)
I [a. u.]
T [K]
I [a. u.]
T [K]

## Slide 4: FWS & ERS Analysis
Global Fitting Model
Lorentzian function
HWHM
Relaxation time
ERS fit:
FWS fit (adapted from H. Grapengeter et al., Colloid Polym. Sci. 1987):
Fitting parameters are shared between different datasets
Notes: These equations assume independent motion and Arrhenius behavior of the described processes.

## Slide 5: FWS Analysis – Regions A + B
EFWS
IFWS shows the need for a low-T process
Q = 1.62 Å-1
IFWS
Results from global fitting
ERS, BS
T = 150 K

## Slide 6: Low-T Analysis - DWF
Cut at 160 K
Get slope from linear fit

## Slide 7: Low-T Analysis - DWF

## Slide 8: Low-T Analysis - DWF
Fitted DWF
EFWS

## Slide 9: Low-T Analysis - DWF
(From fitted DWF)
Rather low, but comparable with confined water systems

## Slide 10: Fit Parameters
Fit parameters for 85% RH sample compared to published results for 8% RH sample at Q14 = 1.62 Å-1
M. Plekhanov et al., J. Phys. Chem. C 2024
Origin | [meV] | [ps] | [μeV]
L1 |  |  | 
L2 |  |  | 
Water |  |  | 
Ligand |  |  | 
Magnetic |  |  | 
Origin |  |  | 
L1 |  |  | 
L2 |  |  | 
Water |  |  | 
Ligand |  |  | 
Magnetic |  |  | 
L1 suggests diffusion, ligand contribution is not excluded
Current work

## Slide 11: Conclusions & Future Directions
Summary Pre-Melting Phase Transition: continuous Arrhenius process is unsuitable
Data Treatment Solution: Splitting into pre- (T < 248 K) and post-transition (T > 258 K) fits; DWF analysis
Outlook Analysis of D2O data to separate water and citrate ligand contributions
Model pre-melting phase transition
MD simulations for a better understanding of surface water dynamics at high RH
• 0.94 Å-1
• 1.31 Å-1 (Bragg peak)
• 1.62 Å-1
EFWS
I [a. u.]
T [K]

## Slide 12: Acknowledgements
IFK and JCNS teams
Mirijam Zobel, Andreas Magerl
DFG (grant nr. ZO 369/3-1)
Markus Appel, ILL
Dieter Richter
Reiner Zorn
Margarita Kruteva
Ralf Biehl
Sascha Ehlert
Thank you!

## Slide 13: FWS & ERS analysis
Citrate-Capped IONPs at 8% RH: “dry” sample
A 3-process model describes the data well in the non-Bragg region.
Q = 1.62 Å-1
M. Plekhanov et al., J. Phys. Chem. C 2024

## Slide 14: FWS & ERS analysis
Citrate-Capped IONPs at 8% RH: “dry” sample
Origin | Parameter | 340 K
Citrate | [meV] | 
 | [meV] | 
Water | [meV] | 
 | [meV] | 
Magnetic | [meV] | 
 | [meV] | 
Origin | Parameter | 340 K
Citrate |  | 
Water |  | 
Magnetic |  | 
Fitted and calculated from global fit at Q = 1.62 Å-1
Q dependence of citrate and
Q2 dependence of water and
M. Plekhanov et al., J. Phys. Chem. C 2024

## Slide 15
Fixed-Window Scans (FWS): • EFWS (ΔE = 0 µeV) & IFWS (ΔE = 3 µeV) from 2 K to 380 K
Energy-Resolved Spectra (ERS): • BS mode, at 2 K, 150 K, 270 K, 300 K, 360 K
Sample information
Truncated octahedra (∼ 6-7 nm), citrate coverage ∼ 2.8 ligands / nm²
Mixed Fe₃O₄/γ-Fe₂O₃ phases: main magnetic Bragg at Q ≈ 1.31 Å-1 (magnetite), minor maghemite peaks at Q ≈ 1.54 Å-1 and 1.74 Å-1

## Slide 16
EFWS () Q4 – Q16
IFWS () Q4 – Q16