## Slide 1: Potential of neutron spectroscopies in studies of complex hydrides for hydrogen storage applications
NAME, title
Olena Zavorotynska, Associate professor
Department of Mathematics and Physics
University of Stavanger, Norway

## Slide 2: Stavanger, Norway
«Three swords» commemorate the historic Battle of Hafrsfjord (y. 872) which united Norway under one crown.

## Slide 3
University of Stavanger
20 years
1 900 employees
12 300 students

## Slide 4: Department of Mathematics and Physics
Materials’ Physics devision
Helge B. Larsen
(Prof.)
Eva Rauls
(Prof.)
Olena Zavorotynska
(Assoc. Prof.)
ab-initio modelling
surface physics, defect physics, heterostructures, amorphous materials
synchrotron techniques: XAS, PXRD
Raman spectroscopy
metal hydrides, surface physics, porous materials, functional oxides
x-ray diffraction
materials physics
crystallography

## Slide 5: Overview
Metal hydrides as hydrogen-carrier media
2. Classification, structure, hydrogen storage properties
3. Applications beyond hydrogen storage
4. Mg(BH4)2 : hydrogen storage and electrolyte
5. Mg(BH4)2 : insights with neutron spectroscopies
6. Summary

## Slide 6: Low H2 density calls for storage and transportation solutions

## Slide 7: Material-based storage as the alternative to the physical storage
materials-based hydrogen storage aims at outperforming the liquid and high-pressure solutions
Scott McWhorter, et al.Moderate temperature dense phase hydrogen storage materials within the US department of energy (DOE) H2 storage program: trends toward future development
Crystals, 2 (2012), pp. 413-445
Metal hydrides (MH) is a very large class of materials that can offer a wide range of working conditions and gravimetric / volumetric hydrogen densities. New compounds, mixtures, composites are being constantly reported.
more favorable storage T, p
avoid liquefaction and pressurization costs
avoid costly insulating tanks
higher volumetric H-energy densities than that in liquid H2

## Slide 8: Hydrides for hydrogen storage
https://www.energy.gov/eere/fuelcells/hydrogen-storage
Saline
hydride
LiH, MgH2, CaH2…
Complex TM
hydride
Mg2NiH4, Mg2FeH6
heavy: low wt% of H (1-2 wt%)
expensive/rare transition metals
operate near RT and at suitable p
fast kinetics of adsorption/desorption
contain plenty of hydrogen per volume

## Slide 9: Hydrides for hydrogen storage
https://www.energy.gov/eere/fuelcells/hydrogen-storage
Saline
hydride
LiH, MgH2, CaH2…
Complex TM
hydride
Mg2NiH4, Mg2FeH6
contain plenty of hydrogen per mass and volume
abundant elements
very stable («bad» thermodynamics)
slow kinetics of H absorption/desorption, complex reaction pathways (complex and chemical hydrides)
hazardous by-products

## Slide 10: MH for hydrogen storage: research directions
New structures and synthesis methods
New composites
Find catalysts / additive and understand their effect on absorption/desorption kinetics and reaction pathways
Nanostructuring / dispersion on porous matrix
Understand the fundamentals of H in solids
Tune / change / enhance thermodynamics and kinetics of H absorption and desorption reactions by:

## Slide 11: MH: new horizons
neutron moderation
Batteries (all solid-state battery, beyond-Li, Mg-battery electrolytes)
thermal storage
heat pumps
smart windows / sensors
purification/separation
superconductivity (near-RT superconductivity was recently achieved in super hydrides)
US department of energy notes that “Metal hydrides (MHx) are the most technologically relevant class of hydrogen storage materials for a wide range of applications …*
* (https://www.energy.gov/eere/fuelcells/metal-hydride-storage-materials)

## Slide 12
Motivation:
avoid flammable organic liquid electrolytes
avoid low-capacity carbonaceous anodes
Results:
Electrolyte:
0.7Li(CB9H10)–0.3Li(CB11H12)
Conductivity:
6.7 × 10−3 S cm−1 at 25 °C – highest among all known SS electrolytes
stable for 300 cycles
All solid-state battery performance:
Notes: One recent result I would like to mention here. It was published just recently by the same group in Tohoku University who published the first paper that I showed you a while ago.
They have prepared this complex electrolyte which exhibited best ever conductive properites for the solid-state electrolyte at room temperature. Also this electrolyte was stable for more than three hundred cycles. They have also assembled the battery call which has shown quite interesting properties for 20 cycles.

## Slide 13: Why are they ionic conductors?
Cation diffusion is facilitated by:
rotational disorder of [BH4]─ (or other anions)
formation of metastable interstitial sites
«paddle-wheel» mechanism of cation mobility similar to that in oxides*
Guzik et al., J of Materials Research, 2019, 877; Matsuo et al., Adv. Energy Mater. 1, 161 (2011); Buchter et al., Phys. Rev. B, 78, 094302 (2008); Remhof et al., Phys. Rev. B, 81, 214304 (2010); M. Jansen et al., Angew. Chem., Int. Ed. 30, 1547 (1991)*

## Slide 14: Mg(BH4)2 for solid-state hydrogen storage
High hydrogen content (14.8 wt%)
Less stable than LiBH4
2-steps decomposition process
From theory: decomposition below 100 °C

## Slide 15: Mg(BH4)2 as electrolyte in batteries

## Slide 16: Research questions addressed with neutron techniques (so far)
Structure (diffraction)
Vibrational properties (INS)
Rotational dynamics of (BH4)- and additives in complexes Mg(BH4)2 · additive (QENS)
Infiltration into porous matrix (SANS)

## Slide 17: Phase polymorphism in Mg(BH4)2
150-200oC
β-Mg(BH4)2 Fddd
β´-Mg(BH4)2 ?
ε-Mg(BH4)2 ?
1.1 – 1.6 GPa
δ-Mg(BH4)2 I41/acd
O. Zavorotynska et al. Int. J. of Hydrogen Energy, 2016, 14387-14403
Y. Filinchuk, R. Cerny, H.Hagemann, Chem. Mater. 2009, 21, 925.
Y. Filinchuk, B. Richter, T.R. Jensen, V. Dmitrivev, V. Chernyshov, H. Hagemann, Angew. Chem. Int. Ed. 2011, 50, 11162.
J.-H. Herr, P.W. Stephens, Y.Gao, G-L. Soloveichik, J.Rijssenbeek, M. Andrus, J.-C. Zhao, Acta Crystallogr. Sect B, 2007, 63, 561
B. Richter, D.B. Ravnsbæk, N. Tumanov, et al. Dalton Trans., 44 (2015), pp. 3988-3996.
Synthesis
γ-Mg(BH4)2 Ia-3d
(porous, high SSA )
α-Mg(BH4)2 P6122
amorphous
ζ-Mg(BH4)2 P3112
Notes: Loads of useful information on structure and related functionality of metal hydrides have have been learnt from neutron studies.
Traditionally it is structure. Neutron diffraction is indispensible to obtain precise positions for hydrogen atoms which for these experiments are substituted by deuterium

## Slide 18: Phase polymorphism in Mg(BH4)2
α-Mg(BH4)2: P 61 2 2
γ-Mg(BH4)2: I a ͞3 d
Notes: Loads of useful information on structure and related functionality of metal hydrides have have been learnt from neutron studies.
Traditionally it is structure. Neutron diffraction is indispensible to obtain precise positions for hydrogen atoms which for these experiments are substituted by deuterium

## Slide 19: Phase polymorphism and phase transitions in Mg(BH4)2
Zavorotynska, et al., Energies 2015, 8, 9173-9190; doi:10.3390/en8099173
In-situ synchrotron XRD (λ = 0.70135 Å) at 3 bar H2
γ-Mg(BH4)2
ε-Mg(BH4)2
β-Mg(BH4)2
ε-Mg(BH4)2
Notes: Phase transitions can be readily observed by in-situ X-ray diffraction as in this examples: RT gamma phase is transformed to the intermediate epsilon, and then to the stable beta-Mg(BH4)2

## Slide 20: Phase polymorphism in Mg(BH4)2
Incoherent INS spectra of β-Mg(BH4)2
Giannasi A. et al. (2010), J. Phys. Chem. A, 114, 2788–2793. Dimitrievska, M., et al. (2016). PCCP 18(36): 25546-25552
Incoherent INS
TOSCA-II, ISIS
BH4 in lattice
H-B-H bending
B-H stretching
Calc.
Exp.
Exp.
Exp.
Calc.
Incoherent INS
FANS, NIST-NCNR
Notes: Loads of useful information on structure and related functionality of metal hydrides have have been learnt from neutron studies.
Traditionally it is structure. Neutron diffraction is indispensible to obtain precise positions for hydrogen atoms which for these experiments are substituted by deuterium

## Slide 21
Comparison to Raman and FTIR / γ-Mg(BH4)2
Dimitrievska, M., et al. (2016). PCCP 18(36): 25546-25552
Vibrational modes in free (BH4)2- (Td)
C2
C3
In solid state (BH4)2- has Cs symmetry and F2, E mode split
INS with no selection rules detects all librations and split bending modes
Stretching modes are better assessed by FTIR/Raman
Notes: Loads of useful information on structure and related functionality of metal hydrides have have been learnt from neutron studies.
Traditionally it is structure. Neutron diffraction is indispensible to obtain precise positions for hydrogen atoms which for these experiments are substituted by deuterium

## Slide 22: Phase polymorphism in Mg(BH4)2
Incoherent INS spectra of β-Mg(BH4)2
Giannasi A. et al. (2010), J. Phys. Chem. A, 114, 2788–2793. Dimitrievska, M., et al. (2016). PCCP 18(36): 25546-25552
Incoherent INS
TOSCA-II, ISIS
BH4 in lattice
H-B-H bending
B-H stretching
Calc.
Exp.
Exp.
Exp.
Calc.
Incoherent INS
FANS, NIST-NCNR
Notes: Loads of useful information on structure and related functionality of metal hydrides have have been learnt from neutron studies.
Traditionally it is structure. Neutron diffraction is indispensible to obtain precise positions for hydrogen atoms which for these experiments are substituted by deuterium

## Slide 23: Mg(BH4)2 for hydrogen storage
Decomposition (H2 release) pathway
H2 release pathway is still unclear
Depends on the starting phase and reaction conditions
Some decomposition phases are amorphous that makes it difficult to distinguish with diffraction methods
FTIR/Raman – broad peaks hampers phase identification
Decomposition occurs above 200 C although theoretically predicted at 80 – 100 C
Theoretical assessment depends on the starting phase – importance for correct structure determination
Partially reversible at an intermediate decomposition step at relatively mild conditions (200 – 300 C, 100 – 150 bar)
Zavorotynska et al. Int. J. of Hydrogen Energy, 2016, 14387-14403
Notes: Loads of useful information on structure and related functionality of metal hydrides have have been learnt from neutron studies.
Traditionally it is structure. Neutron diffraction is indispensible to obtain precise positions for hydrogen atoms which for these experiments are substituted by deuterium

## Slide 24: Mg(BH4)2 as HS medium
Decomposition (H2 release) pathway:
Example of phase identification with INS
H2 release pathway is still unclear
Depends on the starting phase and reaction conditions
Some decomposition phases are amorphous that makes it difficult to distinguish with diffraction methods
FTIR/Raman – broad peaks hampers phase identification
Decomposition occurs above 200 C although theoretically predicted at 80 – 100 C
Theoretical assessment depends on the starting phase – importance for correct structure determination
Partially reversible at an intermediate decomposition step at relatively mild conditions (200 – 300 C, 100 – 150 bar)
Dimitrievska, M., et al. (2016). PCCP 18(36): 25546-25552
Notes: Loads of useful information on structure and related functionality of metal hydrides have have been learnt from neutron studies.
Traditionally it is structure. Neutron diffraction is indispensible to obtain precise positions for hydrogen atoms which for these experiments are substituted by deuterium

## Slide 25: QENS: reorientational dynamics in β-Mg(BH4)2
QENS + DFT
QENS is optimal due to large incoherent H2 scattering cross-section of H
Two thermally activated reorientations of the [BH4]- units, around C2 and C3 axes observed at 120 to 440 K
EC2 = 39 meV, 76 meV; EC3 = 214 meV
Only 15% of [BH4]- were active at 120 K supposedly those close to Mg-Mg axis
QENS finding in close agreement with DFT calculations
Blanchard, D., et al. (2012). "Hindered Rotational Energy Barriers of BH4- Tetrahedra in β-Mg(BH4)2 from Quasielastic Neutron Scattering and DFT Calculations." Journal of Physical Chemistry C 116(2): 2013-2023.
Incoherent QENS
SPHERES (Leibnitz), MARS (SINQ)

## Slide 26: QENS: reorientational dynamics in β-Mg(BH4)2
Blanchard, D., et al. (2012). "Hindered Rotational Energy Barriers of BH4- Tetrahedra in β-Mg(BH4)2 from Quasielastic Neutron Scattering and DFT Calculations." Journal of Physical Chemistry C 116(2): 2013-2023.
Incoherent QENS
SPHERES (Leibnitz), MARS (SINQ)

## Slide 27: INS + QENS: reorientational dynamics in Mg(11BH4)2·3TDF/THF
THF shows positive effect on dehydrogenation but its role is unknown
Vibrational properties of [BH4]- are strongly influenced by the THF environment (INS) (symmetry lowering)
Rotations of [BH4]- around C2 were NOT affected by presence of THF (QENS)
Dimitrievska, M., et al. (2020). PCCP ,22: 368.
Instruments: DCS (QENS), HFBS (QENS)
FANS (INS)
The majority of the studies of Mg(BH4)2 + additives with QENS follow this procedure

## Slide 28: QENS: reorientational dynamics in Mg(BH4)2·additive: correlation with Mg2+ conductivity
QENS + INS // DFT + MD
addition of methylamine significantly speeds up the reorientational frequency of the BH4– anion compared to Mg(BH4)2
NH2 group of the methylamine ligand exhibits much slower reorientation
EIS + PDF + QENS
In amorphous Mg(BH4)2 Mg2+ conductivity is ~102 times higher than in γ-Mg(BH4)2
Local structures are same in 5.1 Å scale
a much larger fraction of activated [BH4] rotations in amorphous Mg(BH4)2 (QENS)

## Slide 29: Hydride dispersion in porous matrix (INS)
Conclusions are based on comparison of INS spectra of bulk hydrides and hydride + porous scaffold composite
Colognesi et al., et al. (2012). JALCOM, 538: 91-99.
INS
TOSCA-II, ISIS
IN4C, ILL

## Slide 30: Infiltration into porous matrix (SANS)
Mg(11BD4)2 in activated carbon scaffold
Infiltration was shown by SANS measurements
Up to 400 °C the nanoconfined particles maintain their size distribution 1-6 nm
decomposition affects only the morphology of the particle surface

## Slide 31: Molecular hydrogen storage in porous complex hydride
Oh, H., et al. (2024). "Small-pore hydridic frameworks store densely packed hydrogen." Nature Chemistry 16(5): 10.
INS + neutron diffraction
H2 and N2 occupy distinctly different adsorption sites: 2.33 H2 and 0.66 N2 / Mg(BH4)2.
Extremally high volumetric density of the molecular H2: 144 g / L
Penta-H2 cluster: some H2 molecules rotate, other have a well-defined orientation and a directional interaction with the framework.

## Slide 32: Summary
H-containing compounds are of special interest for neutron studies due to large neutron scattering cross-sections with H
Structure of hydrides is primarily determined by neutron diffraction
INS has been used to study vibrational properties of hydrides and composites. Advantages: no selection rules, emphasized lattice modes, straightforward calculations of the spectra for assignment, cryostat availability. Disadvantages: no selection rules, low-intensity stretching modes, expensive, large amount of sample, long collection times, long idea – experiment time.

## Slide 33: Summary
QENS studies of rotational dynamics of (BH4)- , effect of additives on the dynamics, correlation between rotations and ionic conductivity
INS, SANS: infiltration into porous matrix
Potential for polarized neutron spectroscopy?

## Slide 34
Thank you for your attention